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HE30TF tubing
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In the past a batch of tubing was found to be defective.  When clamped in the vice a crack was heard.  On examination the tube had cracked right through along its length indicating it was a defective bridge porthole extrusion
Test all tubes by cutting off a 10 mm piece from the end of the tube then crush it to half diameter in two opposite planes in the vice.
If defective the tube will split along its length.
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